REPUBLIC OF TÜRKİYE

GAZIANTEP UNIVERSITY

CIVIL ENGINEERING DEPARTMENT

CE 244 MATERIALS OF CONSTRUCTION

AGGREGATE TESTS

LECTURER

Prof. Dr. Nihat ATMACA

BY

Student Number / Name Surname

Group III

2025-2026 SPRING

DATE OF SUBMISSION

- PURPOSE

- Talk about the aim of the experiments in two or three sentences.

- RESULTS AND CALCULATIONS

Bulk Specific Gravity (TS EN 1097-6:2022):

| Sample | W1 (in the air) (g) | W2 (in the water) (g) | SG |
| --- | --- | --- | --- |
| Crushed Stone (SSD) | 362.36 | 142.35 |  |

Bulk Density (TS EN 1097-3:1999):

| Sample | Wloose (g) | Wcompacted (g) | V (l) | ρloose (g/cm3) | ρcompacted (g/cm3) | Void ratio (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Fine Aggregate: Natural Sand (SSD) | 4132.2 | 4709.3 | 2.4 |  |  |  |

Sieve Analysis and Granulometry Curves (TS EN 933-1:2012):

| Sieve Analysis Results |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sieve size, di (mm) | Fine Aggregate: Natural Sand |  |  | Coarse Aggregate: Crushed Stone No.1 |  |  | Coarse Aggregate: Crushed Stone No.2 | Mixture Aggregate |  |
|  | Amount retained (g) | Amount passed (g) | Percent passed (%) | Amount retained (g) | Amount passed (g) | Percent passed (%) | Percent passed (%) | Percent passed Pm (%) | 100-Pm (%) |
| 31,5 | 0 |  |  | 0 |  |  | 93.0 |  |  |
| 22,4 | 0 |  |  | 0 |  |  | 58.0 |  |  |
| 16 | 0 |  |  | 0 |  |  | 15.0 |  |  |
| 8 | 0 |  |  | 1074.6 |  |  | 1.0 |  |  |
| 4 | 0 |  |  | 420.3 |  |  | 0.0 |  |  |
| 2 | 160 |  |  | 19 |  |  | 0.0 |  |  |
| 1 | 145 |  |  | 0 |  |  | 0.0 |  |  |
| 0,5 | 195 |  |  | 0 |  |  | 0.0 |  |  |
| 0,25 | 220 |  |  | 0 |  |  | 0.0 |  |  |
| 0,125 | 180 |  |  | 0 |  |  | 0.0 |  |  |
| Pan | 80 |  |  | 0 |  |  | 0.0 |  |  |
| Mixture proportions | %30 |  |  | %30 |  |  | %40 | Fineness modulus …………. |  |

- Check if the mixture aggregates are suitable using reference granulometry curves for concrete with a maximum aggregate size of 31,5 mm in TS 802 (March 2016)